## Slide 1
Glove Standards
(EN420, EN388, EN407, EN511, EN374)

## Slide 2
EN 420 – General Requirements for Gloves
This standard defines the general requirements for all protective gloves in terms of construction, fitness of purpose, safety, etc.
- The gloves themselves should not impose a risk or cause injury.
- The pH of the gloves should be as close as possible to neutral.
- Leather gloves should have a pH value between 3.5 – 9.5.
- The highest permitted value for chromium is 3 mg/kg (Chrome VI).
- Specific details of any substance used in the glove which is known to cause allergies must be listed.
- Sized by reference to an agreed common European hand size, for example, minimum length.
Glove Size | 6 | 7 | 8 | 9 | 10 | 11
Minimal Length (mm) | 220 | 230 | 240 | 250 | 260 | 270
Hand Circumference (mm) | 152 | 178 | 203 | 229 | 254 | 279
Hand Length (mm) | 160 | 171 | 182 | 192 | 204 | 215

## Slide 3
EN 388 – Protective gloves against mechanical risks
After EN 420, this standard is the most common found amongst protective gloves. It is tested to multiple different risks, these include Abrasion, Cut, Tear, Puncture, and Impact. Gloves, once tested, are given either a marking or a label which has the standards it has been tested to on, including the scores it achieved.
The pictogram (symbol) for EN 388 is:
Cut (ISO 13997)
Abrasion
Cut (Coup Test)
Tear
Puncture
X.X.X.X.X.X
Impact

## Slide 4
EN 388 – Protective gloves against mechanical risks
Abrasion Resistance:
Samples are cut from the palm of a glove and rubbed against a 180 grit abrasive paper using a “Martindale” type abrasion machine. The number of cycles for the samples to hole is measured.
Number of cycles | 100 | 500 | 2000 | 8000
Level | 1 | 2 | 3 | 4
Cut Resistance (Coup test):
Samples are taken from the palm of a glove and the number of cycles to cut through the full thickness of the test sample by a circular rotating blade, with 5 Newtons of pressure, is recorded. Blade sharpness will vary and is assessed by using the cut test machine to cut through a standard reference fabric. This test is known as the ‘Coup Test’. The cut resistance of the glove is based on a relative index that compares the number of cycles to cut through the glove when compared with the standard fabric.
Cut Index | 1.2 | 2.5 | 5 | 10 | 20
Level | 1 | 2 | 3 | 4 | 5

## Slide 5
EN 388 – Protective gloves against mechanical risks
Tear Resistance:
Samples are taken from the palm of a glove and are torn apart using a standard tensile test machine. The score is based off the Newtons of force required to tear the sample apart.
Newtons of Force | 10 | 25 | 50 | 75
Level | 1 | 2 | 3 | 4
Puncture Resistance:
Samples are taken from the palm of a glove and the force required to penetrate the sample with a defined stylus using a tensile test machine is measured. The score is based off the Newtons of force required to penetrate through the sample.
Newtons of Force | 20 | 60 | 100 | 150
Level | 1 | 2 | 3 | 4

## Slide 6
EN 388 – Protective gloves against mechanical risks
ISO 13997 Cut Resistance (New to 2016):
Traditionally, the level is based on the cut index gained by a test using a rotating blade being drawn along fabric samples until cut-through occurs. This is commonly referred to as the ‘Coup Test’. However, where fabrics have a high resistance to cutting, this test can often create anomalous results due to blunting of the test blade. In such cases, an alternative method specified in EN ISO 13997:1999 is used. The ISO 13997 test runs a straight blade over the sample, replacing the blade after each cut, the Newtons of force applied to the blade is adjustable so that it can give a more accurate level of cut resistance for gloves that naturally blunt blades.
Newtons of Force | ≥2 | ≥5 | ≥10 | ≥15 | ≥22 | ≥30
Level | A | B | C | D | E | F
Impact Resistance (New to 2016):
Other than the fingers, each area where impact protection is claimed shall be tested for impact attenuation by measuring the peak transmitted force. To test the glove, the area of protection is secured over a domed anvil and is impacted at an energy of 5J.
 | Pass | Fail
Level | P | X
*This test is optional unless the blade is blunted testing to the Coup Test, then ISO 13997 is mandatory.
*This test is optional.

## Slide 7
EN 407 – Protective gloves against thermal hazards
EN 407 is divided up into 6 tests and has the pictogram:
Resistance to small splashes of molten metal
Resistance to flammability
Resistance to contact heat
Resistance to convective heat
Resistance to radiant heat
X.X.X.X.X.X
Resistance to large splashes of molten metal

## Slide 8
EN 407 – Protective gloves against thermal hazards
Resistance to flammability:
The glove’s material is stretched and lit with a gas flame. The flame is held against the material for 15 seconds. After the flame is extinguished, the length of time it takes for the material to stop burning or glowing is measured.
Test | Measured In: | Level 1 | Level 2 | Level 3 | Level 4
After-burn time | Seconds | ≤20 | ≤10 | ≤3 | ≤2
After-glow time | Seconds | Infinity | ≤120 | ≤25 | ≤5
Resistance to contact heat:
The glove’s material is exposed to temperatures between +100˚C and +500˚C. The length of time it takes the material on the inside of the glove to increase by 10˚C from the starting temperature (25˚C approx.) is then measured. The minimal amount of time accepted is 15 seconds.
Test | Measured In: | Level 1 | Level 2 | Level 3 | Level 4
Contact Heat | Temp in ˚C after 15 seconds | 100 ˚C | 250 ˚C | 350 ˚C | 500 ˚C

## Slide 9
EN 407 – Protective gloves against thermal hazards
Resistance to convective heat:
The length of time is measured for the heat from a gas flame to increase the temperature of the gloves inside material by 24˚C.
Test | Measured In: | Level 1 | Level 2 | Level 3 | Level 4
Convective Heat | Seconds | ≤4 | ≤7 | ≤10 | ≤18
Resistance to radiant heat:
The glove’s material is stretched in front of a heat source with an effect of 20-40 kw/kvm. The average time is measured for heat penetration of 2.5 kw/kvm.
Test | Measured In: | Level 1 | Level 2 | Level 3 | Level 4
Radiant Heat | Seconds | ≤5 | ≤30 | ≤90 | ≤150

## Slide 10
EN 407 – Protective gloves against thermal hazards
Resistance to small splashes of molten metal:
The test is based on the total number of drops of molten metal required to increase the temperature by 40˚C between the inside of the glove and the skin.
Test | Measured In: | Level 1 | Level 2 | Level 3 | Level 4
Drops of molten metal | Number of drops | ≥5 | ≥15 | ≥25 | ≥35
Resistance to large splashes of molten metal:
Simulated skin is attached to the inside of the glove material. Molten metal is then poured over the glove material. The total number of grams is measured of how much molten metal is required to damage the simulated skin.
Test | Measured In: | Level 1 | Level 2 | Level 3 | Level 4
Molten metal | Gram | 30 | 60 | 120 | 200

## Slide 11
EN 511 – Protective gloves against cold
Resistance to convective cold
Water Permeability
X.X.X
Resistance to contact cold

## Slide 12
Resistance to convective cold:
This is measured based on the transfer of cold through the glove via convection. A model hand heated to body temperature is subjected to a cold room; the resistance to the room’s climatic temperature and also the energy required by the hand to maintain a constant temperature are both measured to arrive at a final score.
EN 511 – Protective gloves against cold
Scored from 0 – 4 (X=not been tested)
Resistance to contact cold:
This measures the how protective the garment is when put into direct contact with a cold object or source. The sample is placed between a warm plate and a cold plate before an extractor fan is used to cool both plates further, the results are then compared to a reference standard and a final level decided.
Scored from 0 – 4 (X=not been tested)
Resistance to water permeability:
These tests ensure that your hands will be completely safe from water seeping in and is simply a pass (1) or fail (0) (X=not been tested) - if the glove cannot withstand water permeating its fabric after 30 minutes of exposure it will fail. Receiving a Level 0 on this test does not necessarily mean these gloves do not perform highly in the other two areas and can still earn them accreditation. All gloves that achieve this standard must also pass at least level 1 of the EN 388 abrasion tests.

## Slide 13
EN 374 – Protective gloves against chemicals and micro-organisms
EN374:
For a glove to be resistant to micro-organisms it must successfully undergo the penetration test and meet at least Level 2. The penetration test consists of the air leak test and the water leak test.
For the Air leak test the glove is immersed in water and the interior of the glove is filled with pressurised air. Leaks are detected if air bubbles emit from the glove.
For the water leak test the glove is filled with a minimum of 1L of water and hung with the fingers facing down. Leaks are detected by any water droplets appearing on the outside of the glove.
Performance Level | Acceptable Quality Level
Level 3 | >0.65
Level 2 | >1.5
Level 1 | >4.0
Performance Level 2 is deemed to be an acceptable
barrier against microbiological hazards.

## Slide 14
EN 374 – Protective gloves against chemicals and micro-organisms
EN374-1:
Resistance to permeation is assessed by measuring the length of time it takes for a chemical to permeate the glove’s material. There are 18 chemicals which are each given a corresponding letter. Depending on if a glove material can resist permeation for 1 chemical at level 1. Or 3, or 6 chemicals on the list to at least Level 2. The glove is
awarded either the type A, B, or C Pictogram and the
corresponding letters for the chemicals are placed
beneath. Other chemicals can be tested but will not
have a corresponding letter.
X
*Pictogram 1
Measured Breakthrough Time | Performance Level
>10 Minutes | Level 1
>30 Minutes | Level 2
>60 Minutes | Level 3
>120 Minutes | Level 4
>240 Minutes | Level 5
>480 Minutes | Level 6
EN374-1:2016/type C
X.X.X
*Pictogram 2
EN374-1:2016/type B
X.X.X.X.X.X
*Pictogram 3
EN374-1:2016/type A
Code | Chemical
A | Methanol
B | Acetone
C | Acetonitrile
D | Dichloromethane
E | Carbon disulphide
F | Toluene
G | Diethylamine
H | Tetrahydrofuran
I | Ethyl acetate
J | n-Heptane
K | Sodium hydroxide 40%
L | Sulfuric acid 96%
M (New addition) | Nitric Acid 65%
N (New addition) | Acetic Acid 99%
O (New addition) | Ammonium Hydroxide 25%
P (New addition) | Hydrogen Peroxide 30%
S (New addition) | Hydrofluoric acid 40%
T (New addition) | Formaldehyde 37%

## Slide 15
This presentation’s intellectual property and design where applicable belongs to: BEESWIFT Ltd, Delta Point, Greets Green Road, West Bromwich, B70 9PL. UK.
For further information please visit www.Beeswift.co.uk
Or contact a sales representative at sales@Beeswift.com